SECTION 5230

MANHOLE COVERS, ROAD GULLY GRATINGS

AND FRAMES FOR DRAINAGE PURPOSES

- SCOPE

- APPLICABLE STANDARDS

- SUBMITTALS

- MATERIAL

- PROTECTIVE COATING

- DESIGN REQUIREMENTS

- QUALITY CONTROL

- MARKING

- MANHOLE COVERS, INSPECTION COVERS AND FRAMES

- ROAD GULLY GRATINGS AND FRAMES

- KERB – TYPE GULLY COVERS AND FRAMES

- LOADING TEST

- MEASUREMENT AND PAYMENT

SECTION 5230

MANHOLE COVERS, ROAD GULLY GRATINGS AND FRAMES FOR DRAINAGE PURPOSES

1.	SCOPE OF WORK

The work to be done under this section of the specifications consists of furnishing all plants, labour, equipment, appliances, material and performing all operations required in connection with supply and installation of C.I cover with frame,  complete as specified herein, as shown on the drawings and or as directed by the Engineer.

All cast iron covers and frame shall be of the sizes and grade (or duty) as specified on the drawings.  The specified size means the clear opening. The cover shall be complete with frame.  Top of cover shall be roughened in an approved pattern.  Locking and lifting arrangement shall also be provided.  The frame shall be well in place at the time of pouring of concrete.  The cover shall tightly fit in the frame.  It shall be air tight and water tight.

## APPLICABLE STANDARDS & SUBMITTALS

Manhole covers with frame		BS-497

- SUBMITTALS

The contractor shall provide samples and literature for manhole & grating covers with frame from approved manufacturers or as directed by the Engineer.

4.	MATERIAL

4.1	The metal used for the manufacturer of castings shall be either:-

a).	flake graphite iron (also called grey iron) of a quality not less than that specified as grade 10 BS 1452: 1961.

b).	Spheroidal or nodular graphite iron or (also called ductile iron) complying with the requirements specified in BS 2789: 1973 for grade 500/7, 600/3 or 700/2, as selected by the manufacturer to suit the design and dimensions of the unit.

4.2	Cast steel gully gratings.  The metal used for the manufacture of cast steel gratings shall comply with the requirements for BS 592 grade: A given in BS 3100: 1967.

4.3 	Bolts.  Bolts supplied for loosely coupling separate sections of covers and grating, shall be steel, hexagon headed, complying with the requirements of BS 4190: 1967 and not less than size M16, complete with hexagon nut:  these shall be provided with means to prevent undue tightening of the unit sections.  Alternative coupling devices, of used, shall be of steel, have a minimum cross sectional area of 140 mm2, and be removable and incapable of undue lightening of loosing.

  - PROTECTIVE COATING

All units shall be supplied coated by dipping, or other equivalent means, using a hot applied coal tar based material.  Alternatively, at the option of the manufacturer, a cold applied black bitumen material may be used.  No coating shall be applied to any casting unless the surfaces of the casting are clean, dry and free from rust.

6.	DESIGN REQUIREMENTS

Products manufactured to the requirements of this standard shall be capable of supporting, without fracture, the following design loads.

| Grade of cover or grating | Design load |  |
| --- | --- | --- |
|  | (KN) | (Tonns) |
| A | 350 | 35.14 |
| B | 150 | 15.06 |
| C | 10 | 1.00 |

The contractor/manufacturer shall verify the design of each type of unit by submitting a sufficient number of prototypes of the loading tests specified in this clause and in Clause 7 below.

7. 	QUALITY CONTROL

  - Quality control tests.  The contractor/manufacturer shall test sample units, by the method given in appendix A of BS specifications 497, for compliance with the requirements given in 7.2

  - Acceptance requirements.  Products shall be deemed to comply with the loading test requirements of this standard if, when tested in accordance with the procedures described in section 12, the following requirements are satisfied.

- Grey iron units sustain the loads specified in 9.3, 10.3 and 11.3 without fractures.

- Ductile iron and cost steel units sustain the loads specified in 9.3, 10.3 and 11.3 without fracture and any resultant permanent set, measured are the midpoint  between any two selected supporting seatings after removal of the test load, is not greater than one five hundredth (0.2 %) of the distance between these selected seatings.

  - Testing of recessed covers.   Recessed covers shall be tested before they are filled with concrete.

### MARKING

All covers, grating and frames shall have clearly cast thereon the number of this British Standard and the appropriate grade, e.g. BS 497, Grade A, and such other markings as may be agreed between the manufacturer and the purchaser.

#### MANHOLE COVERS, INSPECTION COVERS AND FRAMES

  - Grades, Manhole covers, inspection covers and frames complying with the requirements of this British Standard shall be graded as follows:

Grade A	(Extra Heavy duty)

Manhole covers and frames, capable of bearing wheel loads up to 11.50 tones for use in carriage ways.  These covers and frames shall incorporate a permanent non-rock design feature such as triangular point suspension or machined faces.

Grade-B

Class-1	(Heavy duty)

Manhole covers and frames, capable of bearing wheel loads up to 5.00 tones, for use in carriage ways carrying relatively slow moving normal commercial vehicles.  These covers and frames shall incorporate a permanent non rock design feature such as triangular point suspension or machined faces.

Grade-B

Class 2	(Medium duty)

Sealed manhole covers and frames (see 9.4.7) capable of bearing wheel loads up to 5.00 tones, for use in area to which vehicles would have only occasional access (e.g. pedestrian precincts).

Grade-C	(Light duty)

Sealed inspection covers and frames (see 9.4.7) for use in situation inaccessible to motor vehicle.

The duty, weight, test and working load for 600mm circular or square C.I. cover and frame shall be as follows:-

Class/Duty of 			Gross 	      Peak or 		Service

Cover and Frame 	            Weight      Test Load            Working Load

Extra Heavy Weight 	          275-285Kg      35 Ton 		11.5 Ton

Heavy Weight 		          200-210Kg      15 Ton 		 5 Ton

Medium Weight 	          130-140Kg        5 Ton 	            1.5 Ton

Light Weight 			70- 80Kg        1 Ton 	          upto 1 Ton

  - Shape and size.  Only minimum clear opening size and certain frame dimensions are stipulated (see 9.5), shape (.e.g square, rectangular, circular) and size being the product of the individual manufacturer’s design.

The minimum clear opening dimensions that relate to rectangular designs in table 3, 4 and 5 shall be deemed not to be contravened by projections at the corners, required for manufacturing purposes, provided that the resulting reduction of minimum clear opening area does not exceed        15 cm2 at each of the corners.

  - Test loads for quality control purposes (see also Clauses 7 and 12).  The loads and sizes of the bearing blocks for the test specified in clause 7 shall be as follows:

| Grade of cover | Test Load |  | Size of block |
| --- | --- | --- | --- |
|  | Grey iron | Ducting iron |  |
|  | (KN) | (KN) | (mm) |
| Grade-A Manhole covers | 350 | 235 | 300 dia |
| Grade B classes 1 and 2 manhole covers | 150 | 100 | 300 dia |
| Grade C inspection covers | 10 | 7 | 300 dia |

  - Design features

    - Displacement by traffic.  The design of covers shall be such that they cannot be displaced by normal traffic. Grade A and grade B frames of less than 100 mm depth shall be provided with means of additional anchorage (e.g openings and/or holes for anchor bolts in the flange.

    - Drainage and skid resistance.  Covers of solid top type shall be self draining and have a raised pattern, such as chequers, so as to provide a skid resisting surface.

    - Loosening. A recess for a prising bar shall be incorporated in manhole covers unless other means of loosening the cover from the frame are provided.

    - Grade C recessed cover shall be recessed to a clear depth of not less than 28 mm.  The recess shall extend, except for keyway housing and locking pads, to within 25 mm of the outside of the frame at surface level.

    - Keyways.  At least two keyways shall be provided in each complete cover, one in each segment for a double triangular cover.  Closed keyways shall always be provided on grade B Clase-2 and on grade C covers, open or closed keyways may be provided on grade A, on grade B class 1 and on kerb type gully covers.

    - Clearance.  The maximum clearance between cover section and frame, or between section and section, shall be 3 mm (as for gratings).

    - Sealing.  When a manhole or inspection cover unit is described as sealed, unless an alternative method is agreed by the purchaser, the frame shall provide a continuous means of retaining a sealing material.  This standard seal may be of either single or double pattern and the minimum depth of penetration of the cover sealing flange(s) into the frame shall be 10 mm.

    - Locking. Where specified by the Engineer, means shall be provided for locking sealed covers in their frames, without nullifying the seal.  Where locking devices would be rendered ineffective by corrosion, they shall be suitably protected.

    - Ventilated covers.  The total area of ventilation shall be not less than 5% of the minimum clear opening area.  The width of slots shall not exceed 40 mm and their length shall not exceed 125 mm.

  - Specified dimension and details. The dimensions of manhole covers and frames of specified grades and BS reference numbers shall be as given in table 1 to 5

##### Table1.	Grade-A manhole covers and frames

| BS Reference | Minimum clear opening (see 9.2) | Minimum depth of frame | Minimum bedding width of frame) |
| --- | --- | --- | --- |
|  | (mm) | (mm) | (mm) |
| MA-50 | 500 dia | 75 | 75 |
| MA-55 | 550 dia | 75 | 75 |
| MA-60 | 600 dia | 75 | 75 |

##### Table-2	Grade-B class 1 manhole covers and frames

| BS Reference | Minimum clear opening (see 9.2) | Minimum depth of frame | Minimum bedding width of frame) |
| --- | --- | --- | --- |
|  | (mm) | (mm) | (mm) |
| MB1-50 | 500 dia | 75 | 75 |
| MB1-55 | 550 dia | 75 | 75 |
| MB1-60 | 600 dia | 75 | 75 |

##### Table 3.	Grade-B class 2 single seal manhole covers and frames

| BS Reference | Minimum clear opening (see 9.2) | Minimum depth of frame | Minimum bedding width of frame) |
| --- | --- | --- | --- |
|  | (mm) | (mm) | (mm) |
| MB2-50 | 500 dia | 75 | 75 |
| MB2-55 | 550 dia | 75 | 75 |
| MB2-60 | 600 dia | 75 | 75 |
| MB2-60/45a | 600 x 450 | 75 | 75 |
| MB2-60/60a | 600 x 600 | 75 | 75 |
| MB2R-60/45b | 600 x 450 | 75 | 75 |
| MB2R-60/60b | 600 x 601 | 75 | 75 |
| a. Solid top |  |  |  |
| b. Recessed top |  |  |  |

##### Table 4	Grade-C single seal inspection covers and frames

| BS Reference | Minimum clear opening (see 9.2) | Minimum depth of frame | Minimum bedding width of frame) |
| --- | --- | --- | --- |
|  | (mm) | (mm) | (mm) |
| MC1-45/45a | 450 x 450 | 40 | 40 |
| MC1-60/45a | 600 x 450 | 40 | 40 |
| MC1-60/60a | 600 x 600 | 40 | 40 |
| MC1R-45/45b | 450 x 450 | 60 | 40 |
| MC1R-60/45b | 600 x 450 | 60 | 40 |
| MC1R-60/60b | 600 x 600 | 60 | 40 |
| a. Solid top |  |  |  |
| b. Recessed top, See 6.4.5 |  |  |  |

# Table 5	Grade-C double seal inspection covers and frames

| BS Reference | Minimum clear opening (see 9.2) | Minimum depth of frame | Minimum bedding width of frame) |
| --- | --- | --- | --- |
|  | (mm) | (mm) | (mm) |
| MC2-45/45a | 450 x 450 | 40 | 65 |
| MC2-60/45a | 600 x 450 | 40 | 65 |
| MC2-60/60a | 600 x 600 | 40 | 65 |
| MC2R-45/45b | 450 x 450 | 60 | 65 |
| MC2R-60/45b | 600 x 450 | 60 | 65 |
| MC2R-60/60b | 600 x 600 | 60 | 65 |
| a. Solid top |  |  |  |
| b. Recessed top, See 6.4.5 |  |  |  |

### ROAD GULLY GRATINGS AND FRAMES

10.1	Grades. Road gully gratings and frames complying with the requirements of this British Standard shall be graded as follows.

Grade A

Class 1	Gully gratings and frames, capable for bearing wheel loads up to 11.50 tones, for use in carriageways.  These gratings and frames shall incorporate a permanent non rock design feature such as triangular point suspension or machined seating.

Class 2	Gully gratings and frames, incorporating a hinged grating and capable of bearing wheel loads up to 11.50 tones, for use in carriageways.

Grade B	Gully gratings and frames, incorporating a hinged grating and capable of bearing wheel loads up to 5.00 tones, for use in carriageways carrying relatively slow moving normal commercial vehicles.

10.2 	Shape and size.  Two minimum ‘nominal’ widths, 325 mm and 450 mm, with minimum water way area are specified (see 10.5), shape and size being the product of the individual manufacturer’s design (see figure 2* for definition of nominal width).  ( * for figures, see BS-497 standard)

  - Test loads for quality control purposes (see also Clause 7 and 12).  the loads and sizes of the bearing blocks for the purposes of the test specified in clause 7 shall be as follows:-

|  | Test Load |  |  |  |
| --- | --- | --- | --- | --- |
| Grade of grating | ###### Grey iron | Ductile iron | Cast steel | Size of block (see notes 1 and 2) |
|  | KN | KN | KN | (mm) |
| A | 350 | 235 | 235 | 300 x 235 |
| B | 100 | 100 | 100 | 300 x 235 |

NOTE:1	If a non-flat upper surface is specified for a grating (see 7.4.4), the test block shall have a contoured bottom face to mate with the shape of the grating.

NOTE:2	The test block shall be used with the 300 mm side parallel to the kerb face of the gully.

  - Design features

    - Waterway area distribution.  Of the total waterway area, there shall be  minimum of 45 cm2 between the kerb face of the frame and a parallel line 50 mm distant (line X-X in figure 2)* and there shall also be a minimum of 60cm2 between the kerb face of the frame and a parallel line 90 mm distance ((line Y-Y) in figure 2)*.

( * for figures, see BS-497 standard)

    - Slot width and direction. The maximum width of a slot in a grating shall be limited to 40 mm, this figure to include the 3 mm clearance  (see 10.4.3) when this forms an integral part of such a slot.  The predominant direction of slots must be at an angle to the kerb face of between 40o  and  90o .

    - Clearance.  The maximum clearance between grating section and frame, or section and section, shall be 3 mm (see figure 2)*.  The area of such clearance shall not count as part of the minimum waterway area specified in 10.5 nor shall it count as part of the areas as specified in 10.4.1, except where such clearance forms an integral part of an adjacent drainage slot.

( * for figures, see BS-497 standard)

    - Grating surface.  The upper surface of all gratings shall be flat unless otherwise agreed between Engineer and manufacturer.

    - Grating length and width.  The actual length of the grating shall not be less than 325 mm.

    - Displacement by traffic.  The design of gratings shall be such that they cannot be displaced by normal traffic.  Frames of less than 100 mm depth shall be provided with means of additional anchorage (e.g openings and/or holes for anchor bolts in the flange).

    - Hinged gratings.  When designed to hinge open, gratings shall be self supporting in the fully open position.  They shall remain open when the frame is placed on a test slope as indicated below, with the hinge side at the top of the slope.

Type 			Test slope

Hinged at kerb

On road side		1 in 20

Hinged at end		1 in 10

  - Specified dimensions and details.  The dimensions of roads gully gratings and frames of specified grades and BS reference numbers shall be as give in table 6 to 8.

##### Table 6	Grade-A class 1 gully gratings and frames

| BS Reference | Minimum nominal width (see figure 2)* | Minimum area of water way | Minimum depth of frame | Minimum bedding width of frame ** |
| --- | --- | --- | --- | --- |
|  | (mm) | Cm2 | (mm) | (mm) |
| GA1-325 | 325 | 650 | 75 | 75 |
| GA1-450 | 450 | 900 | 75 | 75 |

**	On three sides of grating only, no frame flange on kerb face

*	for figures, see BS-497 standard

##### Table 7	Grade-A class 2 gully gratings and frames

| BS Reference | Minimum nominal width (see figure 3)* | Minimum area of water way | Minimum depth of frame | Minimum bedding width of frame ** |
| --- | --- | --- | --- | --- |
|  | (mm) | Cm2 | (mm) | (mm) |
| GA2-325 | 325 | 650 | 75 | 75 |
| GA2-450 | 450 | 900 | 75 | 75 |

**	On three sides of grating only no frame flange on kerb face

*	for figures, see BS-497 standard

##### Table 8	Grade-B  gully gratings and frames

| BS Reference | Minimum nominal width (see figure 3)* | Minimum area of water way | Minimum depth of frame | Minimum bedding width of frame ** |
| --- | --- | --- | --- | --- |
|  | (mm) | Cm2 | (mm) | (mm) |
| GB-325 | 325 | 650 | 75 | 75 |
| GB-450 | 450 | 900 | 75 | 75 |

**	On three sides of grating only no frame flange on kerb face

*	for figures, see BS-497 standard

11.	KERB – TYPE GULLY COVERS AND FRAMES

11.1	Duty	These covers and frames are for use in the kerbs of carriageways.

11.2	Types	Units shall provide kerb inlet with access cover opening away from the carriageway.  Weir depth (distance from top of cover to top of fixed weir, if any) shall be either 115 mm or 165 mm .

  - Test load for quality control (see also clause 7 and 12).  A load of 150 kN for grey iron units, or 100 kN for ductile iron units, on a rectangular bearing block 300 mm x 235 mm (with the 300 mm dimension parallel to the kerb face) shall be used for the purpose of the test specified in clause 7.

  - Design features

    - Weir length and water way.  The weir length shall be at least 425 mm and a rectangular clearway at least 250 cm2 in area shall be provided above the weir level ( see 11.2), both excluding any debris trap as specified in 11.4.4.

    - Road retaining bar.  Unless otherwise specified by the Engineer, a road retaining bar minimum cross section 35 mm x 25 mm, shall be provided as a standard feature.  It shall be supplied loose so as to provide adjustment to suit the required road level.  Alternatively, a deflector plate may be provided.

    - Cover	 The cover shall be provided with either a keyway(s) for the standard small key or a locking mechanism.  Where the cover may be readily raised without the use of the key or other tool, a locking mechanism shall be provided.  Where a hinge is provided, this shall be at the rear edge of the cover as viewed from the road.  The top shall be self draining and have an adequate raised pattern, such as chequers to provide a slip resisting surface.

    - Debris trap.  A robust grid with horizontal bar(s) or a minimum of two vertical fins shall be provided to act as a debris trap across the open mouth of the unit.

    - Cleaning access.  The opened unit shall provide a minimum rectangular clear opening 400 mm x 250 mm.

  - Specified dimensions.  The dimensions of kerb-type gully covers and frames of specified BS reference numbers shall b as given in table-9

##### Table 9	      Kerb-type gully gratings and frames

| BS Reference | Weir depth | Minimum net weir length | Minimum rectangular clearway | Minimum rectangular clear opening (see 10.4.5) |
| --- | --- | --- | --- | --- |
|  | (mm) | (cm2) | (mm) | (mm) |
| GK-115 | 115 | 425 | 250 | 400 x 250 |
| GK-165 | 165 | 425 | 250 | 400 x 250 |

- LOADING TEST

12.1	Apparatus.	The following apparatus is required

12.1.1	A standard frame to be used as a supporting frame.

12.1.2	Bearing block of the shape and size specified in 9.3, 10.3 and 11.3 as appropriate, of hardwood faced with hard rubber or other resilient material, and sufficiently hard to ensure that the load on the cover of grating is only distributed over the full area of the  block.

12.1.3	A device, preferable a hydraulic testing machine for applying the load.  The device shall be capable of applying a load at least 25% greater than the appropriate load specified in 9.3, 10.3 and 11.3.  If a testing machine is used, it shall comply with the accuracy requirements for grade.  A or grade B testing machines given in BS 1610: 1964.  If any other load measuring device is used it shall be accurate to within 2% of the indicated load.

12.1.4	A measuring device, accurate to 0.1 mm, suitable for indicating deflection measurements on the ductile iron units and cast steel gully gratings.

12.2	Procedure Carry out the loading test by applying the appropriate load specified on 8.3, 9.3 and 10.3 through the bearing block of specified size specified size placed centrally on the section(s) being tested.  For grey iron covers or gratings proceed as described in 12.2.1 for ductile iron covers and grating and cast steel gratings as described in 12.2.2

12.2.1.	Grey iron covers of gratings.  Support the cover or grating in the frame and, using the testing machine or other load measuring device (12.1.3) apply the appropriate load without shock.  Sustain the load for a minimum period of 30 second.

12.2.2	Ductile iron covers and gratings and cast steel gratings.   Support the cover or grating in the frame and take two readings with the measuring device (12.1.4) as follows.

  - Before the load is applied, take an initial reading at a point midway between the two selected supporting seatings to establish a datum point.  Where it is not practicable to make this measurement exactly on the line drawn between the two supporting seatings, it shall be taken on a line parallel to, and as near as possible to, this line.

  - Apply the test load, without shock, five times, sustaining alternating maximum and zero loads for minimum period of 20 seconds then take a second reading at the datum point.

Record the difference between the two readings at the permanent set.

- MEASUREMENT AND PAYMENT

  - Measurement

Measurement of acceptably completed works of cast iron cover with frame will be made on the basis of actual number of cover with frame provided and installed in position as shown on the drawings or as directed by the Engineer.

  - Payment

Payment will be made for acceptably measured quantity of cast iron cover with frame on the basis of actual number quoted in the bill of quantities and shall constitute full compensation for all the works related to the item.