SECTION - 6411

WATER PROOFING/EXPANSION JOINT FILLING

AND BUILTUP ROOFING

1.	SCOPE

2.	SUBMITTALS

3.	MATERIAL

4.	DELIVERY, STORAGE AND HANDLING

5.	EXECUTION

6.	MEASUREMENT AND PAYMENT

1.	SCOPE

The work under this section of the Specifications consists of furnishing all plant, labour, equipment, appliances and materials and in performing all operations in any floor and at any height in connection with installation of insulation, water-proofing & built-up roofing, including water proof treatment to foundations and basement structures complete in strict accordance with this section of the specifications and the applicable drawings and subject to the terms and conditions of the Contract.

2. 	SUBMITTAL

2.1	Shop Drawings: Shop drawings shall be submitted showing layout and all the details for construction.

2.2	Samples of all materials proposed for use under this section, shall be submitted to the Engineer for approval.

3.	MATERIALS

3.1	Bitumen shall be 80/100 grade and Special Industrial Bitumen (SIB) HYCARB A-10 of National Petrocarbon Ltd.

3.2	Polyethylene building film visqueen standard or approved equal. The film shall be 150 (minimum) microns thick.

3.3	Cement and aggregates shall be in accordance with specifications for "Plain and reinforced concrete".

3.4	Flexo-Crete distributed by MGC or an approved equivalent water proofing material shall be used in the thickness of 0.75 mm minimum each coat.

3.5	Bricks shall conform to specifications for "Brick Masonry" and Terracotta tiles shall be imported of Spanish origin and shall conform to relevant specifications provided in Section-6600.

3.6	Sealant to be used in expansion joints and flashings shall be 2 part polysulphide or approved equivalent.

3.7	PVC Geo-membrane as per ASTM standards or approved equal. The membrane shall be 0.25 mm thick.

3.8	For thermal insulation closed cell polyethylene foam bonded sheets manufactured by JUMBOLON shall be used. The thickness of bonded sheets shall be 2” minimum.

4. 	DELIVERY STORAGE AND HANDLING

Materials shall be protected from damage during loading shipment delivery and storage. Non-staining materials shall be used for blocking and packing.

5.	EXECUTION

5.1	PREPARATORY WORK

5.1.1	All scuppers and roof drains shall be placed and metal flashing flanges etc. shall be provided in time to be installed along with the roofing assembly.

5.1.2 	All surfaces, to be treated shall be dust free and dry. Application of roof finishes shall not start unless the preparatory work has been inspected and approved by the Engineer.

5.2 	APPLICATION

5.2.1	Roofing shall not be applied during rain or while surfaces are damp, it shall be applied only to surfaces that are clean and dry.

5.2.2	Mopping of surface with bitumen shall be performed so that the surface shall be completely covered. Coats of bitumen shall be as specified in drawings. All bitumen shall be applied with mops except that the hot surfacing application shall be poured from a dipper.

    - Polyethylene sheet shall be laid in position wherever shown in drawings or specified herein. Where joint is necessary at the side or end of the sheet, this shall be a double weld folded joint made by placing the edges together and folding over twice continuously taking the top edge prior to the application of mud plaster. The Contractor shall protect the sheets from damages during laying and subsequent operation and shall replace at his own cost all damaged sheets to the satisfaction of the Engineer.

    - All surfaces must be moistened before application of waterproofing treatment (Flexo-Crete) and the material shall be applied in strict compliance to recommendations furnished by the manufacturer and the number of coats and their thickness shall be as specified. The Contractor shall protect the applied surfaces from damages during application and subsequent operation and shall redo the application at his own cost to all damaged areas to the satisfaction of the Engineer.

    - PVC Geo-membrane sheet shall be laid in position wherever shown in drawings. Where joint is necessary at the side or end of the sheet, this shall be in strict compliance to recommendations furnished by the manufacturer. The Contractor shall protect the sheets from damages during laying and subsequent operation and shall replace at his own cost all damaged sheets to the satisfaction of the Engineer.

    - Concrete shall be laid in panels, to the desired thickness and slope and shall conform to the requirements of specifications.

    - Terracotta tiles of approved size shall be laid, grouted and pointed flush in cement mortar. The top surface shall be smooth and accurately leveled in accordance with the specified slope. No broken or cracked tiles shall be used.

    - For thermal insulation closed cell polyethylene foam bonded sheets manufactured by JUMBOLON or an approved equivalent shall be laid in places as designated on drawings or as directed by the Engineer.

5.3 	WATER PROOFING & BUILT UP ROOFING

5.3.1	To Retaining Walls.

The water proofing treatment to Reinforced Concrete Walls shall be done in the following manner as indicated on the drawings or as directed by the Engineer.

a)	¾" thick minimum cement plaster mixed with approved water proofing agent.

b) 	2 coats of MGC flexocrete to concrete surfaces with 0.75 mm minimum thickness of each coat.

c)	4-½" thick brick masonry with 1:5 cement sand mortar.

5.3.2	Over Roof Terraces

The water proofing treatment to reinforced cement concrete roof slabs designated as Terraces shall be done in the following manner as indicated on the drawings or as directed by the Engineer.

a)	One layer of PVC Geomembrane 0.25 mm thick properly lapped (at least 4" wide overlap) and sealed as per the recommendations of the approved manufacturer.

b) 	1st layer of polyethylene sheet lapped and joints sealed.

c)	2” thick Thermal insulation closed cell polyethylene foam bonded sheets manufactured by JUMBOLON shall be laid as per Engineers instructions. Joints between the sheets/overlaps shall be treated as per Manufacturer’s recommendation.

d)	2nd layer of polyethylene sheet lapped and joints sealed.

e)	2½" thick average (2" thick min) Reinforced Concrete Class 'C' laid in slope.

f) 	Terracotta tiles of Spanish origin set in 1:3 cement sand mortar and pointed in 1:2 cement sand grout.

5.3.3	Over External Paved Areas

The water proofing treatment to reinforced cement concrete roof slabs designated as paved areas shall be done in the following manner as indicated on the drawings or as directed by the Engineer.

a)	2" thick Concrete Class 'C' with approved waterproofing agent.

b) 	2 coats of MGC Flexo-Crete or an approved equivalent to concrete surfaces with 0.75 mm minimum thickness of each coat.

5.4	WATER PROOFING TREATMENT IN FOUNDATION SUB-STRUCTURES, UNDER FLOORS.

a)	Bitumen Painting

All concrete surfaces directly in contact with earth shall be bitumen painted shall be thoroughly cleaned of any accretion, dust, dirt etc. by scraping, wire brushing or as directed by the Engineer. The surface shall be primed with a coat or asphalt oil used at the rate of not less than 1 gallon /100 square feet. Two coats of hot bitumen paint shall be applied at the rate of 20 lbs/100 Sft. each coat. The first coat shall be allowed to dry for about 6 hours before applying the second coat. During operation of painting great care shall be taken to avoid air bubbles. The manufacturers shall be taken to avoid air bubbles. The manufacturer's instructions and Engineer's directions shall be followed.

b)	PVC Geo-membrane (Water Proofing Membrane)

PVC Geo-membrane shall be laid in position wherever shown on the Drawings.

The material shall be laid over the prepared surface at the levels and position in the areas shown on the Drawings. Where joint is necessary at the side or end of a sheet, this shall be as per the recommendation of the manufacturer. The Contractor shall protect the film sheets from damages during laying and subsequent operation and shall replace at his own cost all damaged film sheets to the satisfaction of the Engineer.

Manufacturer's recommendations and instructions along with the sample of material shall be submitted to the Engineer for his approval.

PVC Geo-membrane on vertical surfaces shall be protected by the construction of 4½" thick masonry wall and on horizontal surfaces it shall be protected/covered by placement/laying of 2" thick cement concrete 1:4:8.

5.5		Not Used

5.6	CURING

Tiles after laying, grouting and flush pointing shall be kept wet throughout for at least 7 days.

6. 	MEASUREMENT AND PAYMENT

6.1	General

Except otherwise specified herein or elsewhere in the Contract Documents, no measurement and payment will be made for the under mentioned specified works related to the relevant items of the Bills of Quantities. The cost thereof shall be deemed to have been included in the quoted unit rate of the respective items of the Bills of Quantities.

The rates quoted by the Contractor in the Bill of Quantities shall include work to be executed under these specification in any floor and at any height except where otherwise specifically stated in the relevant item of Bill of Quantities and the Contractor shall not be entitled to any claim or claim any compensation on this account.

6.1.1	All preparatory work, scrapping, scratching, cleaning, cant strips, gravel strips, etc.

6.1.2	Formwork

6.1.3		Concrete Class ‘C’, etc.

6.1.4	Coats of bitumen.

6.1.5	Flexo-Crete, Geomembrane, Thermal insulation, Polyethylene sheets, etc. including laps/overlaps.

6.1.6	Terracotta tiles/brick work.

6.2	Water Proofing & Built-up Roofing

6.2.1   Measurement

Measurement of acceptably completed works respective type of water proofing & built-up roofing will be made on the basis of net actual area in square feet provided and installed in position as shown on the Drawings or as directed by the Engineer.

6.2.2   Payment

Payment will be made for acceptable measured quantity of respective type of water proofing & built-up roofing on the basis of unit rate per square feet quoted in the Bills of Quantities and shall constitute full compensation for all the works related to the item.

6.3	Bitumen Painting/Coating

6.3.1   Measurement

Measurement of acceptably completed works of bitumen painting/coating will be made on the basis of net actual area in square feet provided and applied in position as shown on the Drawings or as directed by the Engineer. Area receiving painting/coating shall only be measured once, irrespective of the number of coats applied.

6.3.2	Payment

Payment will be made for acceptable measured quantity of bitumen painting/coating on the basis of unit rate per square feet quoted in the Bills of Quantities. The unit rate shall include all cost of surface preparation and shall constitute full compensation for all the works related to the item.