- SECTION - 3000

- STRUCTURAL STEEL WORKS

- SCOPE

- APPLICABLE STANDARDS

- SUBMITTALS

- MATERIAL

- CONNECTIONS

- EXECUTION

- INSPECTION AND TESTS

- MISCELLANEOUS STEEL WORKS

- MEASUREMENT AND PAYMENT

1.	SCOPE

The work covered by this section, consists of supply of all material, labour, plant, equipment and appliances including welding, bolts, nuts, washers, anchor bolts, embedded parts etc, fabrication, erection and painting in accordance with the specifications and as per drawings and as directed by the Engineer.

2.	APPLICABLE STANDARDS

Latest edition of the following standards are relevant to these specifications wherever applicable:

AISC	Code of standard practice

AISC	Specifications for Design, Fabrication and Erection of Structural Steel for Buildings.

# AISC	Specifications for structural joints using ASTM A325 or A490 Bolts.

## ASTM	Specifications for materials

AISC/	Guide to shop painting of structural steel

SSPC

AWS	Specifications for welding of steel structures

BS 449	Use of structural steel in Buildings

3. 	SUBMITTALS

Design drawings shall be prepared by the Engineer and supplied to the Contractor. These shall contain main dimensions, sizes of members, typical details of joints.

Workshop drawings shall then be prepared by the Contractor from the design drawings supplied and submitted to the Engineer for approval.

4. 	MATERIAL

All the components shall be sound and free from injurious matter, cracks, air-holes, blows, wounds, scales, spitted grains and blunt rises. Except otherwise stated in the drawings, the material specifications shall conform to the following. Wherever necessary the Contractor may use equivalent alternative material subject to approval of the Engineer.

4.1 	STRUCTURAL STEEL

Structural steel for structures shall conform to the requirements of ASTM A-36 or equivalent

4.2	STEEL SHEETS & PLATES

Steel sheets and plates, where required, shall conform to the requirements of BS 1449 “Steel Plates, Sheet and Strips”.

4.3 	STEEL FORGING

Steel forging shall conform to the requirements of ASTM A235.

4.4 	STEEL CASTING

Steel casting shall conform to the requirements of ASTM A27.

4.5 	WELDING

Welding Electrodes for manual shielded metal arc welding shall conform to AWS A 5.1 latest edition or the A 5.5 latest edition. Equivalent locally manufactured electrodes may be used subject to the approval of the Engineer.

4.6	STEEL BOLTS

Except where otherwise shown in the Drawings, the steel bolts shall conform to the applicable requirements of ASTM A307 “Specification for Low Carbon Steel Externally and Internally Threaded Standard Fasteners.”

4.7	COMMON BOLTS, ANCHOR BOLTS, NUTS AND WASHERS

Common Bolts, Anchor Bolts, Nuts and Washers Bolts and Nuts shall conform to the requirements of ASTM A 307.

4.8 	HIGH STRENGTH BOLTS

High strength carbon steel bolts including nuts and washers shall conform to the requirements of ASTM A325 latest editions and of AISI B18.2

4.9 	WASHERS

Cut Washers: Shall be of structural grade steel and shall conform to the dimension of the manufacturer's regular standard for plain washers for the size of bolts used.

4.10 	CAST IRON

Shall conform to the requirements of latest edition of ASTM A 48.

5.	CONNECTIONS

  - DESIGN OF CONNECTION

All connections shall be designed and detailed for forces shown on the drawings, if any or 50% of the effective capacity of the member, whichever is greater.

Shop connections may be welded or bolted. Field connections shall be bolted unless noted otherwise on design drawings.

5.2	INSTALLATION OF BOLTS

High strength bolts shall be installed in accordance with AISC “Specifications for Structural Joints using ASTM A 325 or A 490 bolts”.

5.3	MINIMUM SPACING OF BOLTS

The distance between centers of bolt holes shall not be less than 3d, where d is the diameter of the bolt in inches.

5.4	MINIMUM EDGE DISTANCE

The minimum edge distance i.e. center of standard hole to edge of connected part shall be as given in the table below:

| NOMONAL BOLT DIAMETER (INCHES) | ### AT SHEARED EDGES (INCHES) | AT ROLLED EDGES OR PLATES, SHAPES OR GAS CUT EDGES (INCHES) |
| --- | --- | --- |
| 1 / 2 | 1.5 TIMES THE DIAMETER OF BOLTS | 3 / 4 |
| 5 / 8 |  | 7 / 8 |
| 3 / 4 |  | 1 |
| 7 / 8 |  | 1 – 1 / 8 |
| 1 |  | 1 – 1 / 4 |

5.6	ALLOWABLE STRESSES

Allowable design stresses for structural steel members and their connections, including temporary bracings and shorings shall be in accordance with AISC Specifications.

6. 	EXECUTION

6.1	FABRICATION

The Contractor shall notify the Engineer about any problems or doubts/errors discovered in the drawings for clarification/rectification well in time to prevent any fabrication errors. Fabrication shall not be commenced until approval has been obtained from the Engineer.

6.1.1 	Straightening of Material

Rolled material, before being worked upon must be straightened within tolerances by ASTM specifications A6 Straightening, necessarily shall be done by mechanical means or by the application of a limited amount of localized heat. The temperature of heated areas, as measured by approved methods, shall not exceed 1100F for A 514 steel or 1200F for other steels.

6.1.2 	Cutting

As far as possible cutting must be done by shearing, Oxygen cutting shall be done where shear cutting is not possible and shall preferably be done by Machine. All edges shall be free from gauges, notches or burs. If necessary the same shall be removed by grinding.

Metal sections shall be well formed, to shape and size, with sharp line or angles. Shearing and punching shall leave clean, true lines and surfaces. The metal sections shall be thoroughly straightened by methods that will not injure it, before being laid off or worked in any way. The members shall be so straightened that they are not, more than 1/16”, away from a straight plane in either direction, for the full length of members. All members shall be so cut and formed that they can be accurately assembled without being unduly cracked, strained or forced into position.

6.1.3 	Holes Punching Drilling

Holes shall be punched where thickness of the material is not greater than the diameter of bolt + 1/8". Where the thickness of the material is greater the holes shall either be drilled or sub-punched and reamed to size. The die for all sub-punched holes and the drill to all sub-drilled holes shall be at least 1/16" smaller than the nominal diameter of the rivet or bolt. Holes for A514 steel plates over 1/2" thick shall be drilled.

6.1.4 	Welding

a)	General:

The execution and inspection of welding will be done in accordance with the provisions of the American welding society code for welding in Building construction, D1.0. No welding for piping/electrical supports shall be made transversely to any tension flanges of trusses, beams or columns.

b)	Automatic sub-merged Arc Welding:

For all built-up members, i.e. sections fabricated from plates and flat bars or compound rolled sections, plate and box girders, where long continuous, welding is to be done, should be executed by Automatic submerged Arc Welding process in accordance with relevant AWS specifications.

c)	Maximum and minimum size and lengths of fillet welds shall be in accordance with AISC specifications.

Surface to be welded shall be free from loose scale, slag, rust, grease, paint or any other foreign matter except mill scale, which withstands vigorous wire brushing.

d)	Tolerances

- A variation of l mm is permissible in the over all length of members with both ends finished for Contact bearing. The bearing surfaces prepared to a common plane by milling.

- Members without end finished for contact bearing which are to be framed to other steel parts of the structure shall have a variation from detailed length not greater than 1/8" for length over 30 feet and not greater than 1/16” for length.

- Members with ends finished for contact bearing shall have a variation 1/32” in the over all length.

6.2	TEST ASSEMBLY

    - After fabrication and before galvanization or painting, test assembly of complete Structural Components shall be done on the shop floor as directed by the Engineer.

    - Each test assembly will be inspected by the Engineer and will be dismantled only after his approval in writing

6.3	SURFACE PREPARATION/PAINTING

6.3.1 	Surface Preparation

a) 	All structural steel material i.e. rolled steel sections, plates, pipes, flat bars, chequered plates shall be cleaned free from loose scale, rust, burrs slag, etc. by means of sand blasting.

6.3.2	Painting

a)	Immediately after surface preparation all material shall be given one prime coat of rust preventive paint.

b) 	After fabrication one shop coat of prime paint and then one coat of enamel paint shall be applied.

c) 	One final coat of enamel paint shall be applied after erection of all components.

d) 	The type of primer and enamel paints to be applied shall be as specified on the drawings and the thickness of each coat of the paint shall be in accordance with the specifications of the paint manufacturer.

e) 	All other requirements for the specified paint system shall be in accordance with the paint manufacturer's specification / recommendations.

f) 	The Contractor shall use the best quality of the type of paint specified and shall get the same approved by the Engineer.

g) 	Steel work/Surfaces not to be painted

i) 	Steel work to be encased / embedded in concrete or surface in contact with concrete or grout shall not be painted, but shall be given a cement wash after sand blasting.

- Machined finished surfaces shall not be painted but shall be coated with rust preventive compound, (approved by the Engineer) immediately after finishing. Such surfaces shall also be protected with wooden pads or other suitable means for transportation. Unassembled pins, keys, and bolt thread shall be greased and wrapped with moisture resistant paper.

- Contact surfaces of connections using high strength bolts in friction type connections shall not be painted. Such surfaces of all components after fabrication shall be cleaned free of all paints, grease, burrs slag by means of sand blasting. No coating whatsoever shall be applied to these surfaces. The surface roughness for high strength friction grip bolts is a very important factor and the components therefore will not be erected unless approved by the Engineer.

6.3.3	Zinc Coating

Components should be galvanized after complete fabrication i.e. welding, drilling etc. The process should consist of removal of rust and mill scale by pickling in hydrochloric acid or sulphuric acid followed by water wash and pre-fluxing in tanks containing zinc ammonium chloride and then fluxing with ammonium chloride. The fluxed components should then be passed through a drying oven prior to immersion in a bath of virtually pure molten zinc.

Wherever specified by the Engineer, zinc coating shall be applied in a manner and of a thickness and quality conforming to the requirements of ASTM A123 Standard Specifications for zinc (hot galvanized) coating on products fabricated from rolled, pressed and forged steel shapes, plate bars and strips.

6.4	ERECTION

    - Bracing

The structure shall be carried up true and plumb within the limits defined in the AISC code of standard practice. Temporary bracing shall be introduced wherever necessary to take care of all loads of which the structure may be subjected including the equipment and the operation of the same. Such bracings shall be left in place as long as required for safety.

6.4.2	Alignment

Bolts tightening as specified by ASTM A 325 shall not be done at site during erection until the structure has been fully aligned and leveled.

6.4.3	Joints using High Strength Bolts

All structural joints using high strength bolts shall be executed and inspected in accordance with “AISC Specification for structural joints using ASTN A 325 or A 490 bolts”.

6.4.4	Stubs

Stubbs of trusses before being embedded in concrete shall be erected in position timely aligned using stub setting templates.

7. 	INSPECTION AND TESTS

7.1 	Manufacturer's Work Test Certificate for all material used shall be furnished by the contractor for Engineer's scrutiny and approval.

7.2 	Rolling tolerance of all shapes and profile according to AISC shall be in accordance with the provisions of the American Society for Testing and Materials Designation A.6. The Contractor shall check these before being worked upon and these shall be rejected if found not within limits.

7.3 	The Contractor shall arrange for analysis and test of all material rolled locally at a testing laboratory selected by the Engineer.

7.4 	Inspection of Welding.

The inspection of welding shall be performed in accordance with the American Welding Society specifications, as directed by the Engineer.

7.5 	Rejection

Materials or workmanship not in reasonable conformance with the provisions of these specifications shall be rejected at any time during the progress of the work or the completion and erection at site.

8.	MISCELLANEOUS STEEL WORKS

8.1	General

The work covered shall include furnishing, fabricating, installing and painting miscellaneous steel work including the following:

    - Steel doors and windows

    - G.I. Flashings

    - Steel pipe handrail

    - Steel embedded plates anchor bolts and other miscellaneous items

    - Steel protection angles and channels

    - Structural Steel Trusses

The Contractor shall submit shop drawings for each item showing in sufficient detail the material, its fabrication, surface preparation and other relevant information so as to conform to the applicable requirements of relevant clauses of these specifications for Engineers Approval. After the approval of drawing the Contractor shall erect a mock-up sample showing exactly the finished item as it will be fabricated/erected. Only after the approval of the mock-up sample the Contractor shall start the fabrication of items to be installed in place. Any proposed deviation due to field conditions and availability of local material shall be submitted to the Engineer for approval.

9.	MEASUREMENT & PAYMENT

9.1 	General

Except otherwise specified herein or elsewhere in the Contract Documents, no measurement and payment will be made for the under mentioned specified works related to the relevant items of the Bill of Quantities. The cost there of shall be deemed to have been included in the quoted unit rate of the respective items of the Bill of Quantities.

The rates quoted by the Contractor in the Bill of Quantities shall include works to be executed under these specifications in any floor and at any height.

9.1.1	Nuts, bolts, screw, rivets, heads, fillets, welds welding rods, locks, rollers, rolling tracks, pivot hinges, etc.

9.1.2 	Anti-corrosive prime coat.

9.1.3	Cleaning with sand blasting.

9.1.4	Painting.

9.1.5	Embedding/fixing of steel pipe hand rail in concrete work and wooden covering.

9.1.6	All hardware in steel doors, locks, hold fasts, etc.

9.1.7	All metal embedded parts, metal fittings and fixtures required for the operational process.

    - Providing 2 hour fire resistant doors, UL listed fabricated from 16SWG MS sheet and the core filled with heavy density foam injected polyurethane of low U factor (< .069) and full width door frame fabricated from 14 SWG M.S sheet including painting etc. complete in all respects as per per design, approved shop drawings/mock-up samples of the type FRD1.

    - Glazing in steel door/windows including seals and gaskets and providing/fabricating louvers.

    - Epoxy primer to internal surfaces of door frame and shutter including frame.

9.2	Steel Doors & Windows

9.2.1	Measurement

Measurement of acceptably completed works of respective types of Steel Doors & Windows will be made on the basis of net actual area in square feet fabricated and installed in position as shown on the Drawings or as directed by the Engineer. Net area will be measured in accordance with plastered masonry opening in between jambs and plastered head and bottom of shutter.

9.2.2	Payment

Payment will be made for acceptable measured quantity of respective types of Steel Doors & Windows on the basis of unit rate per square feet quoted in the Bill of Quantities against respective item and shall constitute full compensation for all the works including all hardware & fittings like locks, tower bolts, push plates etc. as per details shown on drawings.

9.3	Steel Handrail

9.3.1	Measurement

Measurement of acceptably completed works of respective types of Steel Hand railing will be made on the basis of actual length in feet fabricated & installed in position as shown the drawings or as directed by the Engineer.

9.3.2	Payment

Payment will be made for acceptable measured quantity of respective types of Steel Hand railing on the basis of unit rate per feet quoted in the Bills of Quantities and shall constitute full compensation for all the works related to the item.

9.4	Structural Steel Trusses

9.4.1	Measurement

Measurement of acceptably completed works of structural steel trusses will be made on the basis of number of metric tons of structural steel provided & erected in position as shown the drawings or as directed by the Engineer.

9.4.2	Payment

Payment will be made for acceptable measured quantity of structural steel trusss on the basis of unit rate per metric ton quoted in the Bills of Quantities and shall constitute full compensation for all the works related to the item.